A spectrometer records intensity within fixed, evenly spaced wavelength intervals (dλ). However, due to the inverse relationship between wavelength and energy, evenly spaced data intervals in wavelength are unevenly spaced in energy. The area under the uncorrected wavelength curve does not strictly conserve the photon flux.

To rigorously quantify the amplified spontaneous emission (ASE) contribution and determine lasing thresholds, edge-emission spectra were processed using a custom Python algorithm. Raw spectra recorded in the wavelength domain Iλ were first converted to the energy domain. To account for the inverse relationship between wavelength and energy E∝λ-1, a Jacobian transformation was applied to the spectral intensity:

IE=Iλ⋅λ2hc

This correction is essential to preserve the integrated photon flux and prevent spectral distortion characteristic of broad organic emission bands.1

The pure ASE signal was isolated by subtracting the spontaneous emission (photoluminescence, PL) background. A reference PL line shape was obtained from the sample emission well below the lasing threshold. For each high-fluence spectrum, this reference shape was scaled to match the intensity of the spectral wings (regions unaffected by spectral narrowing) and subtracted in the energy domain. The resulting "pure" ASE signal was then integrated over the emission band (IASEE) to yield the total ASE intensity. While integration was performed in the energy domain for physical accuracy, spectral narrowing (FWHM) is reported in wavelength units for comparison with standard literature.

1.	Mooney, J. & Kambhampati, P. Get the Basics Right: Jacobian Conversion of Wavelength and Energy Scales for Quantitative Analysis of Emission Spectra. J. Phys. Chem. Lett. 4, 3316–3318 (2013).